## Slide 1: MIT 3.022 Microstructural Evolution in Materials 5: Diffusion
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: (Inter)diffusion
“Diffusion is the net movement of molecules or atoms from a region of high concentration (or high chemical potential) to a region of low concentration (or low chemical potential) as a result of random motion of the molecules or atoms.” – Wikipedia (after my edits )

## Slide 3: Self-diffusion
Migration of atoms in the absence of concentration gradient
Can be characterized using radioactive tracing

## Slide 4: Microscopic diffusion mechanisms
Vacancy mechanism
(Substitutional self-diffusion)
Interstitial mechanism

## Slide 5: Microscopic diffusion mechanisms
Vacancy mechanism
(Substitutional interdiffusion)
Interstitial mechanism

## Slide 6: Interstitial diffusion
Atom vibration frequency:
Frequency of successful hops:
Energy
harmonic potential
Notes: The probability of an harmonic oscillator having energy greater than E_a is given by summing up the occupation probabilities over all levels with higher energy, which gives exp(-E_a/kT)

## Slide 7: Interstitial diffusion
Number of atoms hopped from plane 1 to 2 per unit time and per unit area:
1
2
Similarly, the flux from 2 to 1 is:
The net diffusion flux is:
Fick’s 1st law
Diffusivity (unit: m2/s)
Notes: While the model here assumes a simple cubic structure, it applies to octahedral interstitial diffusion in FCC as well

## Slide 8: Interstitial diffusion
Atom vibration frequency:
Frequency of successful hops:
Typical value estimation:
Energy
harmonic potential
hn
Photon
at room temperature
at 1,000 °C

## Slide 9: Interstitials in FCC crystals
Number of octahedral interstitial sites per unit cell: 4

## Slide 10: Interstitials in FCC crystals
Spacing between octahedral sites:
a
at 1,000 °C
Data from E.A. Brandes and G.B. Brook (Ed.) Smithells Metals Reference Book, 7th ed., 1992.
Notes: C in gamma-iron is an example of octahedral interstitial diffusion

## Slide 11: Deriving Fick’s 2nd law from Fick’s 1st law
1-d case: a rod with a constant cross-section area A
  Concentration of the diffusing atom: C(x, t)
  Diffusion flux:
A
x
C(x, t)

## Slide 12: Deriving Fick’s 2nd law from Fick’s 1st law
Divide the rod into many small (virtual) sections dx
Diffusion flux at the junctions between sections:
A
x
x + dx
Flux entering the section dx
Flux exiting the section dx

## Slide 13: Deriving Fick’s 2nd law from Fick’s 1st law
Net change of the amount of diffusant in the section over a period of dt :
x
x + dx
Amount of diffusant entering the section dx
Amount of diffusant exiting the section dx

## Slide 14: Deriving Fick’s 2nd law from Fick’s 1st law
Net change of the amount of diffusant in the section over a period of dt :
Concentration change rate of the diffusing species:
Fick’s second law (note the sign)
Useful for solving non-steady-state diffusion problems

## Slide 15: Point source diffusion
At t = 0, an amount q of diffusing species is placed on a plane of unit area at x = 0
Diffusion length
  A measure of how far the diffusing species has propagated in time t

## Slide 16: Step concentration diffusion
Initial concentration distribution:
Solution:
where
Error function
Error function

## Slide 17: Diffusion from an extended source
Initial concentration distribution:
Solution:

## Slide 18: Diffusion from an extended source
http://www.mathworks.com/matlabcentral/fileexchange/38088-diffusion-in-1d-and-2d
1-D diffusion from an extended “box” source

## Slide 19: Diffusion from an extended source
http://www.mathworks.com/matlabcentral/fileexchange/38088-diffusion-in-1d-and-2d
2-D diffusion from an extended “box” source

## Slide 20: Diffusion into a plate
Initial concentration distribution:
Solution:

## Slide 21: Example 1: making hams and bacons
Diffusion coefficient of salt in pork ~ 10-9 m2/s
How long does it take to salt a meat slice of 3 mm thickness?
J. Agric. Food Chem. 53, 7814 (2005).
Finite element modeling of salt diffusion using Fick’s 2nd law
© unknown

## Slide 22: Example 2: doping semiconductors
Diffusion doping
Ion implantation
p-Si
P4O10 gas
Mask
Mask
n-channel
p-Si
Mask
Mask
n-channel
P ion

## Slide 23: Example 2: doping semiconductors
Emitter diffusion
Furnace anneal:
4POCl3 + 3O2 → 2P2O5 + 6Cl2
2P2O5 + 5Si → 5SiO2 + 4P
In-line process:
2H3PO4 → P2O5 + 3H2O
2P2O5 + 5Si → 5SiO2 + 4P
Standard silicon solar cell manufacturing process

## Slide 24: Example 3: chemical strengthening of glass
Adv. Mater. 23, 4578 (2011)
© Corning

## Slide 25: Example 3: chemical strengthening of glass
Ion exchange in salt bath
Interdiffusion process
  Kinetics limited by slow-moving ion species
  Compressive strain impedes diffusion
Typical case depth in soda-lime glass: 25 to 35 mm
Only applies to alkali/alkali earth glasses
Int. J. Appl. Glass Sci. 1, 131 (2010)

## Slide 26: Thermodynamic driving force for diffusion
Average velocity of a diffusing species A
Thermodynamic driving force
For an ideal solution of A
Einstein relation

## Slide 27: Summary
Mechanisms of diffusion
  Vacancy & interstitial mechanisms
Microscopic model of diffusion:
Fick’s 1st law and 2nd law
Solutions to common diffusion problems
Examples of diffusion process
Einstein relation
for ideal solution

## Slide 28: List of symbols
T – temperature
k – Boltzmann constant (1.38 × 10-23 m2 kg s-2 K-1)
m – mass of an atom
K – effective spring constant of the potential well where an atom is located
h – Planck constant (6.626 × 10−34 J·s)
n – vibrational frequency of an atom
nh – frequency of successful hops of an atom
Ea – activation energy of atomic hopping
J – diffusion flux of atoms

## Slide 29: List of symbols
n1 / n2 – number of atoms per unit area on plane 1/2
x – coordinate along the x-axis
a – hopping distance (distance between neighboring interstitial sites for interstitial diffusion)
C – number concentration of atoms (i.e. number of atoms per unit volume in 1/m3)
D – diffusivity, diffusion coefficient
Z – number of nearest neighboring interstitial sites
a – lattice constant (note the difference with a )
t – time
A – cross-sectional area

## Slide 30: List of symbols
d – diffusion length
– interdiffusion coefficient
vA – average velocity of diffusing species A
MA – mobility of diffusing species A
FA – driving force of diffusion acting on species A
mA – chemical potential of diffusing species A
mA,0 – chemical potential of diffusing species A at a standard reference state
xA – atomic fraction of species A