## Slide 1: MIT 3.071 Amorphous Materials 15: Characterizing the Amorphous State
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2
 | Technique | Information
Structure | X-ray/electron/ neutron diffraction | Crystallinity, pair distribution function, medium range order
 | X-ray absorption spectroscopy (XAS) | Local structure, electronic state
 | Raman spectroscopy | Phonon spectra, structural clusters
 | Nuclear magnetic resonance (NMR) | Local atomic configurations
Glass chemistry | Atomic emission spectroscopy (AES) | Elemental composition
 | Energy-dispersive X-ray spectroscopy (EDX) | Elemental composition
 | Infrared spectroscopy | Chemical bonding, impurity concentration, optical absorption
 | X-ray photoelectron spectroscopy (XPS) | Valence state of constituents, electron density of states

## Slide 3
 | Technique | Information
Thermal analysis | Differential thermal analysis (DTA) | Glass transition temperature (Tg), crystallization (Tx)
 | Differential scanning calorimetry (DSC) | Glass transition temperature (Tg), crystallization (Tx)
 | Thermogravimetric analysis (TGA) | Chemical decomposition
 | Thermomechanical analysis (TMA) | Thermal expansion, softening point, glass transition (Tg)
Electrical properties | Temperature-dependent electrical conductivity measurement | Conduction mechanism, activation energy, density of states at Fermi level (for VRH)
 | Impedance spectroscopy (AC conductivity) | Conductivity, dielectric constant
 | Electron paramagnetic resonance (EPR) | Defects (e.g. dangling bonds)

## Slide 4
 | Technique | Information
Mechanical and rheological behavior | Indentation | Hardness
 | Ultrasonic wave propagation | Elastic modulus
 | Fracture toughness test | Fracture toughness
 | 3/4-point bending test | Elastic modulus, flexural stress
 | Viscometry | Viscosity
Optical properties | UV-Vis spectroscopy | Optical attenuation, Tauc gap
 | Ellipsometry | Refractive index dispersion, attenuation (k > 0.001)
 | Prism coupling | Refractive index (bulk and thin film), optical attenuation
 | Optical fiber/waveguide transmission | Optical attenuation (thin films with k < 0.001)
 | Photoluminescence | Defect states

## Slide 5: Diffraction techniques
Photo 51, X-ray diffraction pattern of DNA
Image courtesy:
Raymond Gosling
& Rosalind Franklin

## Slide 6: Diffraction techniques
Full 3-D X-ray structure factors of Photosystem I, a protein complex
Image courtesy:
Thomas White, CFEL

## Slide 7: X-ray diffraction (XRD)
Amorphous background
Crystals:
Strong scattering
Localized, intense peaks
Glass:
Weak scattering
Broad scattering background across the entire reciprocal space
Appl. Phys. Lett. 102, 082404 (2013)

## Slide 8: X-ray diffraction in solids
Assumptions:
Approximate incident and diffracted X-ray as mono-chromatic plane waves
Elastic scattering: wavelength of X-ray remains the same after scattering
Neglect X-ray attenuation in the solid sample
Incident wave
Diffracted wave
Sample
rm : position vector of atom m

## Slide 9: X-ray diffraction by a single atom m
Complex amplitude of incident wave:
Field amplitude of the incident wave at rm :
Complex amplitude of wave scattered by atom m:
Sample
E : field amplitude of incident X-ray
ki : wave vector of incident X-ray
ks : wave vector of scattered X-ray
fm : scattering factor of atom m
Q = ks - ki : scattering vector
Incident wave
Diffracted wave

## Slide 10: X-ray diffraction in solids
Total scattered amplitude from the sample :
Total scattered intensity:
Sample
S (Q) : (static) structure factor
N : total number of atoms in the sample
Incident wave
Diffracted wave

## Slide 11: X-ray diffraction in crystals
The condition for a Bragg peak to appear is:
or:
The Bragg peak intensity scales with:
where the sum is over all atoms in a unit cell
T. Proffen, Characterization of Materials using the PDF
Unit cell: the repeating unit of a crystal

## Slide 12: Quantitative description of glass structure
Structural descriptions of amorphous materials are always statistical in nature
Pair distribution function (PDF): g(r)
  Consider an amorphous material with an average number density of atom given by:
  The number density of atoms at a distance r from an origin atom is given by
  When
  When
N : number of atoms V : material volume

## Slide 13: PDFs of ideal (hard sphere) crystals vs. glasses
g(r)
r
1st coordination shell
2nd coordination shell
g(r)
r
1
0

## Slide 14: Mathematical description of PDF
Probability density for finding an atom at r :
Probability density for finding an atom pair at r and r’ :
Pair distribution function:
Homogeneous solid
Homogeneous, isotropic solid
Notes: The definition follows r→0, g→0 and r→∞, g→1

## Slide 15: Structure factor of isotropic amorphous solids
where
In isotropic solids structure factor is related to the Fourier transform of PDF
Notes: In general, the particle positions are not fixed and the measurement takes place over a finite exposure time and with a macroscopic sample (much larger than the interparticle distance). The experimentally accessible intensity is thus an averaged one.

## Slide 16: Debye scattering equation
Isotropic amorphous media:
The inverse transform:
where
XRD spectra can be used to infer PDF of isotropic amorphous solids

## Slide 17: Solving PDF from experimental XRD spectra
Raw XRD data
Data correction
Structure factor normalization
Transform to real space
Data from T. C. Hufnagel, Johns Hopkins University

## Slide 18: Solving PDF from experimental XRD spectra
Raw XRD data
Data correction
Structure factor normalization
Transform to real space
Data from T. C. Hufnagel, Johns Hopkins University

## Slide 19: Solving PDF from experimental XRD spectra
Raw XRD data
Data correction
Structure factor normalization
Transform to real space
Data from T. C. Hufnagel, Johns Hopkins University
Scattered intensity oscillates around the coherent independent scattering at large Q values

## Slide 20: Solving PDF from experimental XRD spectra
Raw XRD data
Data correction
Structure factor normalization
Transform to real space
Data from T. C. Hufnagel, Johns Hopkins University
Structure factor oscillates around unity at large Q values

## Slide 21: Solving PDF from experimental XRD spectra
Raw XRD data
Data correction
Structure factor normalization
Transform to real space
Data from T. C. Hufnagel, Johns Hopkins University

## Slide 22: Solving PDF from experimental XRD spectra
Sources of error
  S(Q) data truncation error
  X-ray photon shot noise
  Finite resolution
Mitigation strategies
  Use Mo (lKa = 0.71 Å) or Ag (lKa = 0.56 Å) sources instead of Cu source (lKa = 1.54 Å)
  Use synchrotron sources
  Increase collection time
PDFGetX2 homepage
J. Appl. Cryst. 37, 678 (2004)
Determination of Pair Distribution Functions (PDF) from Bruker

## Slide 23: Electron and neutron diffraction
Electron diffraction
  Much smaller wavelength (e.g. l ~ 2 pm for 300 keV electrons)
  Small spot size (e.g. in the case of SAED)
Neutron diffraction
  Interacts with nuclei rather than electrons
  Can discriminate neighboring elements or isotopes
  Can detect light elements
Amorphous Ta2O5
Crystalline Ta2O5
Electron diffraction patterns
Class. Quantum Grav. 27, 225020 (2010)

## Slide 24: Raman spectroscopy
When asked about his inspiration behind the Nobel Prize winning optical theory, Raman said he was inspired by the "wonderful blue opalescence of the Mediterranean Sea" while he was going to Europe in 1921.

## Slide 25: Raman spectroscopy
Raman scattering: inelastic interaction of photons with phonons
  Photon – phonon = Stokes line
  Photon + phonon = anti-Stokes line
laser-detect.com/technology-methods/

## Slide 26: (Confocal) micro-Raman system
Bright field microscopy
(Confocal) Raman spectroscopy
“Confocal Raman Spectroscopy,” Micro and Nano Technologies Ch. 7, 141-161 (2017)
Raman Microscope
Confocal micro-Raman spectroscopy: depth resolution at the expense of signal strength

## Slide 27: Raman spectra of amorphous materials
Amorphous materials typically have broad Raman peaks
  Dispersion of local structures and phonon energy
  Breakdown of selection rule
Raman spectrum of c-Si
Raman spectrum of As2S3 glass

## Slide 28
Probing phase transition kinetics in PCM
In-situ Raman probing concurrently reveals PCM structure and heater temperature
Adv. Photonics Res. 3, 2200202 (2022)

## Slide 29
Probing phase transition kinetics in PCM
In-situ Raman probing concurrently reveals PCM structure and heater temperature
Adv. Photonics Res. 3, 2200202 (2022)

## Slide 30
Probing phase transition kinetics in PCM
In-situ Raman probing concurrently reveals PCM structure and heater temperature
Adv. Photonics Res. 3, 2200202 (2022)

## Slide 31
Probing phase transition kinetics in PCM
Boson peak

## Slide 32
Measuring TTT diagrams of PCMs
A facile method for experimental quantification of true TTT diagram in PCMs
Crystallization
Adv. Photonics Res. 3, 2200202 (2022)

## Slide 33: Calorimetry (thermal analysis)
Notes: https://zhuanlan.zhihu.com/p/30794181

## Slide 34
Differential Scanning Calorimetry (DSC) | Differential Thermal Analysis (DTA)
Both techniques involve a sample and an inert reference with known heat capacity both undergoing controlled heating or cooling | 
Heating rate is kept constant for both the sample and the reference, and heat flow to the sample minus heat flow to the reference is recorded | Both the sample and the reference undergo identical thermal cycle and temperature difference between sample and reference is recorded
Reference
Heater
Sample
Heater
Computer control to ensure identical heating rate
Reference
Sample
Heater
Thermal couples record temperature difference

## Slide 35: Differential scanning calorimetry of glass materials
Temperature
Endothermic
Exothermic
Differential heat flow
Glass transition
Crystallization
Melting
Steady state
Area under a DSC peak is proportional to the heat released or absorbed during a phase change
Notes: Sometimes the direction of the vertical axis is flipped

## Slide 36: Glass transition regime behavior in DSC
Cooling rate: 10 °C/s
Varying reheating rate
10 °C/s
1 °C/s
0.1 °C/s
10 °C/s
1 °C/s
0.1 °C/s
Shape of DSC curve at the glass transition regime depends on heating rate and the sample’s thermal history

## Slide 37: Differential thermal analysis of glass materials
Temperature
Exothermic
Endothermic
Temperature difference
K : thermal conductance
Glass transition
Crystallization
Melting
Steady state

## Slide 38: Evaluation of glass forming ability
FOM for glass stability:
Hruby coefficient
Addition of Si increases glass melt viscosity and improves glass forming ability
Czech. J. Phys. B 22, 1187 (1972)
DTA

## Slide 39: Ultrafast DSC using on-chip heater & sensor

## Slide 40: Ultrafast calorimetry for material analysis
Crystal growth rate in Ge2Sb2Te5
Nat. Mater. 11, 279 (2012)

## Slide 41: Summary
Diffraction
  Debye diffraction equation: relation between structure factor and PDF in homogeneous, isotropic amorphous solids
  Solving PDF from experimentally measured XRD spectra: corrections and normalization
  X-ray, electron, and neutron diffraction
Raman spectroscopy
  Broad Raman peaks: phonon energy dispersion
Thermal analysis
  DSC vs. DTA: data interpretation
  Glass transition regime behavior