## Slide 1: MIT 3.156/3.46 Photonic Materials and Devices 8: Optical Scattering
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: References
Principles of Nano-optics, Ch. 12
Electromagnetic Wave Theory, Ch. 6
  J. A. Kong, Wiley & Sons
Light Scattering by Small Particles
  H. van de Hulst, Dover Publications
Absorption and Scattering of Light by Small Particles
  C. Bohren and D. Huffman, Wiley-VCH

## Slide 4
The Lycurgus Cup

## Slide 5
Optics & Photonics News 21, 42-48 (2010)

## Slide 6: How to see around corners
Nat. Commun. 3, 745 (2012)

## Slide 7: Rayleigh theory of optical scattering
Small particles (a << l): quasi-static approximation
The fields inside (E1) and outside (E2) the sphere may be found from the scalar potentials and
a
z
r
E0 (constant)
e1
e2
The initially uniform field
Is distorted by introduction of the sphere
q
(potential )

## Slide 8: A sphere in a uniform static field: the solution
Laplace’s equations in source-free domains:
Boundary conditions:
Solution:

## Slide 9: Field of an electric dipole
Dipole moment:
If the charges are embedded in a uniform unbounded medium with permittivity e2 , then the potential at any point P is given by:
-q
q
r-
r+
r
z
P
q
-
+
d
e2
Ideal (Hertzian) dipole:

## Slide 10: A sphere in a uniform static field: the solution
Electric potential inside and outside the sphere:
A sphere in an static field is equivalent to an ideal dipole
Dipole moment:
Dipole polarizability:

## Slide 11
e1 = 2.2, e2 = 1
e1 = 10, e2 = 1
http://wiki.4hv.org/index.php/Dielectric_Sphere_in_Electric_Field
Field lines
Equipotentials

## Slide 12: Scattering by small spherical particles
The field of an oscillating dipole
Far-field radiation: scattered field in the quasi-static limit
static field
(near-field)
induction field
(near-field)
radiation field
(far-field)

## Slide 13: Rayleigh scattering (a << l)
Particle
Scattering: induced dipole radiation
Scattered sunlight is highly polarized at a scattering angle of 90° (q = 0°)
|Es|
p
E
H
k
p
Scattered field

## Slide 14: Rayleigh scattering (a << l)
Total scattered power (linearly polarized light):
Scattering cross-section ss and scattering efficiency Qs :
Short wavelength light is preferentially scattered
(dimensionless number)
Notes: The scattered light intensity scales with the scatterer’s volume square due to coherent scattering.

## Slide 15: Rayleigh scattering in gas and glass
Density fluctuation results in non-zero Rayleigh scattering
S. Shibata et al., "Prediction of Loss Minima in Infrared Optical Fibers," Electron. Lett. 17, 775 (1981).
Notes: In a uniform medium scattering from different parts of the medium cancels out due to destructive interference, resulting in zero total scattering

## Slide 16: Scattering by small spherical particles (cont’d)
The particle polarizability diverges when
In practical materials, polarizability is always a finite number due to the non-vanishing imaginary part of e1
Significantly enhanced scattering at the dipole resonance wavelength when
Localized surface plasmon resonance (LSPR): enhanced collective oscillation of free electrons
t

## Slide 17: Optical absorption and extinction of spheres
Absorption cross-section sa :
Extinction = scattering + absorption
The contribution to extinction due to optical absorption is more significant for smaller nanoparticles
Optical absorption is also significantly boosted at the dipole resonance wavelength

## Slide 18: Extraordinarily large optical absorption cross-section at the LSPR wavelength
Field lines of Poynting vector around an aluminum sphere at the LSPR resonance wavelength of 141 nm where Qa = 18 (left) and at a non-resonant wavelength of 248 nm where Qa = 0.1 (right).
Absorption and Scattering of Light by Small Particles, C. Bohren and D. Huffman, Wiley-VCH

## Slide 19: Field enhancement at LSPR resonance
a = 30 nm Ag NP
dipole resonance
a = 60 nm Ag NP
quadrupole resonance
J. Phys. Chem. B 107, 668-677 (2003).

## Slide 20: Different conventions and unit systems
Sometimes, unit conversion in electromagnetism can be tricky
According to the convention we use here:
In some books and papers, polarizability is defined as:
In Gaussian unit system:
“I like the metric system. My weight in kilograms is so much less than my weight in pounds.”

## Slide 21: Beyond the Rayleigh theory
Classical modifications
Geometric effects: non-spherical particles
Nanoshells and ellipsoids in the quasi-static limit (a << l)
Discrete Dipole Approxi-mation (DDA)
Finite size effects
Modified Long Wavelength Approxi-mation (MLWA)
Multi-pole expansion: high order Fröhlich modes
Mie scattering theory
Surface damping: mean free path limitation
Quantum plasmon resonance
Quantum effects

## Slide 22: Nanoshells in the quasi-static limit
Nanoshell polarizability
Nanoshell dipole resonance:
Geometrically tunable resonant l
r2
r1
core
shell
where
Au-coated Au2S nanoshells
Averitt et al., J. Opt. Soc. Am. B, 16, 1824-1832 (1999).

## Slide 23: Ellipsoids in the quasi-static limit
Surface of ellipsoid:
For incident field polarized along the x-axis:
where
For incident field with random polarization:
C. Noguez, J. Phys. Chem. C 111, 3806-3819 (2007).
Absorption and Scattering of Light by Small Particles, C. Bohren and D. Huffman, Wiley-VCH

## Slide 24: Discrete Dipole Approximation (DDA)
Represented the arbitrary shaped particle as a cubic lattice of N polarizable small subunits (<< l) with polarizability asu
Induced electric dipole moment of each subunit:
asu is given either by the Clausius-Mosotti relation with the radiative reaction term or the Doyle expression
C. Dungey and C. Bohren, "Light scattering by nonspherical particles: a refinement to the coupled-dipole method," J. Opt. Soc. Am. A 8, 81-87 (1991).
E. Purcell and C. Pennypacker, "Scattering and absorption of light by nonspherical dielectric grains," Astrophys. J. 186, 705-714 (1973).

## Slide 25: Discrete Dipole Approximation (DDA)
Local electric field at the i th subunit is the sum of external field E0 and the dipole field Eij (i ≠ j) of all other subunits at the location ri of the i th subunit
Solve the 3N coupled linear equations for and cross-sections of the particle
A list of DDA computer codes
where

## Slide 26: Modified Long Wavelength Approximation (MLWA)
In MLWA, radiative reaction effect and dynamic depolarization are taken into account by adding a radiative correction field term:
Redshift of LSPR peak in larger particles
where
“The discrete dipole approximation and its application to interstellar graphite," Astrophys. J. 333, 848 (1988).
“Enhanced fields on large metal particles: dynamic Depolarization,” Opt. Lett. 8, 581-583 (1983).
Resonance condition:

## Slide 27: Multi-pole expansion
-
+
+
Monopole
Dipole
-
+
-
+
Quadrupole
-
+
-
+
-
+
-
+
Octupole
Expanding the scattered field by the particle into high order spherical harmonics: radiation by multi-poles
Quadrupole scattering intensity scales with quadrupole polarizability b
Dipole term
Quadrupole term
quadrupole resonance when

## Slide 28: Quadrupole LSPR
Quadrupole resonance
Dielectric constant of Ag
Dipole resonance
a = 30 nm Ag NP
dipole resonance
a = 60 nm Ag NP
quadrupole LSPR
Redshift of dipole resonance peak in a =
60 nm particles due to depolarization (MLWA)
a = 60 nm Ag NP
a = 30 nm Ag NP

## Slide 29: Mie scattering (a ~ l)
Mie theory deals with scattering by isotropic spheres or cylinders with radii a in a homogeneous medium
Scattering efficiency
l / 2a
Polystyrene microspheres in water
J. Appl. Phys. 105, 023110 (2009).
Qs → 2 :
extinction paradox
ss → l -4

## Slide 30: Scattering field pattern by a dielectric sphere
l / a = 20
l / a = 4
l / a = 1
Forward scattering is pronounced in Mie scattering
Plots generated using an online Mie Scattering Calculator

## Slide 31: Mie scattering in optical fibers
l / 2a
Power factor h
Mie scattering by crystalline precipitates
Crystal size estimated based on wavelength dependence of scattering loss
T. Katsuyama and H. Matsumura, J. Appl. Phys. 76, 2036 (1994).

## Slide 32: Electron mean free path limitation in nanoparticles
In metal particles smaller than the mean free path of conduction electrons in bulk metal, the mean free path is limited by collisions with the particle boundary
Drude-Sommerfeld model:
Surface damping mainly increases the imaginary part of permittivity
where is the electron velocity at the Fermi surface
is the mean free path for collisions at the surface
For Ag NPs:
U. Kreibig et al., J. Phys. F, 4, 999 (1974).
Notes: In the last equation, a is given in nm and the equation applies to 405 nm wavelength

## Slide 33: Quantum plasmon resonance
Blue shift of LSPR peak in small (a < 5 nm) metal nanoparticles
Discrete energy levels due to the small number of atoms in a particle
Each transition corresponds to a new bound electron oscillation term in the Lorentz-Drude model
Energy band
2a
E

## Slide 34: Quantum plasmon resonance
Blue shift of LSPR peak in small (a < 5 nm) metal nanoparticles
Discrete energy levels due to the small number of atoms in a particle
J. Sholl et al., Nature 483, 421-428 (2012).

## Slide 35: Applications of LSPR in metal nanoparticles
Small resonance mode volume
  Refractive index sensing: cavity perturbation scales inversely with mode volume
Local field enhancement
  Absorption enhancement in solar cells
  Surface Enhanced Raman Scattering (SERS)
Coupling between metal nanoparticles

## Slide 36: Dark field imaging for scattering measurement
True color image of gold nanorods (red) and gold nanospheres (green)
Phys. Rev. Lett. 88, 077402 (2002).

## Slide 37: Single protein molecule detection
“Single Unlabeled Protein Detection on Individual Plasmonic Nanoparticles,” Nano Lett. 12, 1092-1095 (2012).

## Slide 38: Surface Enhanced Raman Spectroscopy
Raman scattering
  Raman scattering is characterized by “its feebleness in comparison with the ordinary scattering” – C. Raman
  Raman scattering cross sections are typically 14 orders of magnitude smaller than those of fluorescence
SERS: dramatic enhancement of Raman signal on the surface of noble metal nanostructures
  Chemical enhancement factor: ~ 100
  Electromagnetic enhancement factor: 104 up to 1011
Electromagnetic Enhancement Factor (EF):
Chem. Phys. Lett. 423, 63-66 (2006).

## Slide 39: Surface Enhanced Raman Spectroscopy
Field enhancement is most significant at small gaps and sharp tips: the “lightning rod” effect
Phys. Rev. E 62, 4318-4324 (2000). Nat. Photonics 5, 83-90 (2011).
Nano Lett. 5, 119-124 (2005). Chem. Commun. 47, 3769-3771 (2011).
Dimers
Trimers
Bowtie
Nanocrescent

## Slide 40: SERS substrates and “hot spots”
The majority of Raman signal is generated by molecules at locations where the field intensity peaks: hot spots
Self-assembly and top-down fabrication
EF up to 1015
Challenges:
  Hot spot areal density
  Statistical fluctuation
Anal. Chem. 77, 338A-346A (2005).
Hot spot
Phys. Rev. Lett. 76, 2444 (1996).
Science 275, 1102 (1997).

## Slide 41: SERS substrates and “hot spots”
The majority of Raman signal is generated by molecules at locations where the field intensity peaks: hot spots
Self-assembly and top-down fabrication
EF up to 1015
Challenges:
  Hot spot areal density
  Statistical fluctuation
Phys. Rev. Lett. 76, 2444 (1996).
Science 275, 1102 (1997).
Nano Lett. 8, 2423 (2008).

## Slide 42: Coupling between nanoparticle resonances

## Slide 43: Coupling between nanoparticle resonances
Longitudinal mode: field from neighboring particles reinforces each other
(red shift of resonance)
Transverse mode: field from neighboring particles opposes each other
(Blue shift of resonance)
Brongersma et al., Phys. Rev. B 62, R16356 (2000).

## Slide 44: A molecular ruler
Single particle
Dimer
Nat. Biotechnol. 23, 741 (2005)
Red shift
With 40 nm particles and a 0.1 nm spectral resolution, it is possible to measure particle separations with 1 nm resolution

## Slide 45: List of symbols
a – spherical particle radius
l – wavelength
E0 – incident (applied) electric field amplitude
E1 / E2 – electric field amplitude inside / outside the particle
F1 / F2 – electric potential inside / outside the particle
e1 / e2 – permittivity inside / outside the particle
r – radial coordinate
q – angular coordinate
q – electric charge

## Slide 46: List of symbols
p – electric dipole moment
d – spacing between charges
a – dipole polarizability
V – volume of scatterer
E – electric field (vector)
H – magnetic field (vector)
k – wave number
k – wave vector
Ps – scattered power
m0 – vacuum permeability

## Slide 47: List of symbols
ss – scattering cross-section
Qs – scattering efficiency
sa – absorption cross-section
sext – extinction cross-section
g – damping coefficient
w – angular frequency of oscillating electric field
wp – plasma frequency
vF – electron velocity at Fermi surface
L – mean free path for electrons due to surface collision
er – relative permittivity (dielectric constant)

## Slide 48: List of symbols
Vmode – resonant mode volume
w0 – angular frequency of light at resonance
Dw0 – resonant frequency change due to perturbation
EF – SERS enhancement factor
lE – Raman excitation wavelength
lS – Raman scattering (Stokes) wavelength